Environmental efficiency as generating factor to enhance productivity - Presentation of the results obtained in a ceramic industry from Ceará State

Cândido H. A. Bezerra a, Josimeire A. Gomes, Ms. b, Kassandra M. A. Morais c, Irani C. Mattos, Dr. d e Rossana B. Silveira Ms.e

a. SENAI-CETAE, Fortaleza/Ce, chbezerra@sfiec.org.br

b. Universidade Federal do Ceará, Fortaleza/Ce, josimeireag@hotmail.com

c. SENAI-CETAE, Fortaleza/Ce, kmmorais@sfiec.org.br

d. Universidade Federal do Ceará, Fortaleza/Ce, ic-mattos@uol.com.br

e. SENAI-CETAE, Fortaleza/Ce, rsbarros@sfiec.org.br

Abstract

The research was carried through in the Cajazeiras Ceramics, industry of the ceramic sector situated in Cascavel-Ceará. The main products produced and commercialized for the company are structural blocks of prohibition, flagstone and blocks. The main substance used cousin is the clay. Effluent liquids, solid residues and atmospheric emissions during the productive activities are generated. The solid residues are generated from the loss of materials for defect in the finished product. A production of more than 2500 milheiros of blocks damaged per year is esteem. The consumption of water, raw material, energy and of solid residues for product had been defined as indicating ambient with the objective to identify the consumption for produced ceramics block, besides identifying the economic loss generated by wastefulness of blocks damaged in the production. With this analysis some alternatives for minimização of the production of residues, effluent had been suggested and emissions inside of the Program of Cleaner Production, such as, Modification in the product, Modification of technology, I reuse and recycling, Compostagem, Alterations in the process, among others. From the evaluation of the raised data the company was divided by sectors (preparation, drawing and burn) for identification of chances and/or problems, plan of action and strategies, barriers and necessities, beyond the identification of the priority level. Had the inadequate use of boquilha the drawing process of the ceramic blocks presented an index of retrabalho verified in up to 30%. With the equipment exchange for boquilhas new and balanced a decrease in the index of re-work in 12% was verified, generating one better exploitation of the natural resources and energy and consequently better indices of productivity and prescription. Associated the technological improvement of the equipment exchange of boquilha, a survey of impurities was carried through that allowed to the planning of a handling of the extration and preparation of the clay most adequate, allowing the clay entrance in the cleaner productive process of resulted impurities and this form providing better in the production. Through surveys in I lease was evidenced that the use of simple door more generates a consumption of 0,08m³/milheiro of the one than with the use of double doors in the ovens hoffmans. With relation to the ambient improvements it is had: Lesser consumption of firewood for produced part, to the end of one year we will have an area of 36Ha of bushes of bioma caatinga that they had not been deforested, considering that 1ha of bush of bioma caatinga produces 52m³ of native firewood (given of the FIERN), providing a lesser ambient impact of that the previous a implantation of the Program of Cleaner Production.

Key words: Cleaner production, ambient impact, solid residues, generation of effluent.